Lab #3	Equilibrium Phase Diagrams

Background  ------

# Definitions

Phase – chemically and structurally homogenous portion of microstructure e.g. a solid solution

Component – distinct chemical substance which makes up the phase (element or compound) e.g. copper and nickel

Phase Diagram – any graphical representation of the state variables associated with microstructures; map of the different possible phases at a given temperature and pressure

State variables – variables which can influence microstructure, e.g. temperature, pressure, and composition (i.e. the ratio of components)

Engineers can alter and set the state variables to establish a particular microstructure – and thereby influence the mechanical properties of the material.

Equilibrium phase diagrams – everything in equilibrium conditions, i.e. stable state (temperature, pressure, etc.) – all chemical reactions are complete

Phase Diagrams

Example: H2O – one component phase diagram

Can use the phase diagram to determine how to go from one phase to another –

e.g.	1. From A to B without a liquid phase

2. From A to B with a liquid phase

Two component phase diagram – two completely soluble components

liquidus – line above which everything is liquid

solidus – line below which the system is solid

tie line – horizontal line connecting the two phase compositions

Lab-----------

Phase Diagram for bismuth and tin (Bi-Sn) – (a binary system)

Melting points

100% Bi		271 degrees C

100% Sn		231 degrees C

50/50 Bi-Sn		139 degrees C

There is a melting point depression with impurities –

What happens when you add salt to water?

Why add anti-freeze to your car?

Key points:

1.  Melting points of pure compounds

2.  Melting point of eutectic (L ( S)

3.  Phase fields

i)

 – Sn with Bi impurities (bct)

 – Bi with Sn impurities (rhombic)

ii) field composed of phases to left and right (middle region)

4.  Liquidus and solidus

- Solubility limit – if you increase the %Bi at constant temp in the Liquid phase, then you get  precipitate – e.g. sugar in water

- Grain structure

Phase percentages and compositions

Tie line – Lever rule

Given a state (%Bi and temp) can find percent phase composition and L composition

For example 1500 C and 20% Bi

Horizontal line intersecting L and S

Finish

Example: steel  - 		freeze a lock and it becomes brittle – goes into a new phase. Lock maker needs to account for these conditions when selecting materials for locks.

Slow vs. fast cooling

Control material properties by processing methods

Composition curves

# Text boxes

Temp 0C

Pressure

1 atm

100

0

## Gas

## Liquid

Solid

Triple point – three phases

Equilibrium lines – both phases

A

B

Temp

% weight A

A

100%

B

0%

L+S

## L

## S

## solidus line

## liquidus line

## melting point of B

## melting point of A

## S

## L

B

A

Temp

X

T

state point

comp. of S at T

comp. of L at T

### system

composition

tie line

L

L+

L+



S



L

L+S

L+S

S

S

S

Temp

0

%NaCl or antifreeze